## Slide 1
Woncosa Capillary

## Slide 2
  Use
  The Capillary is used for all types of bonding machine in the
  semiconductor assembly process.
  The main purpose of capillary here is to connect Chip Pad and
  Lead Frame by moving the wire through its hole.
  Importance
Capillary is...
  The Capillary is very important for successful wire bonding on the chip and lead frame respectively.
  For this reason, it requires all the manufacturers to have a very delicate and sensitive technology involved in making a capillary in deep consideration of bond-ability and Capillary itself
  Furthermore, the Capillary are supposed to be in good shape in and out without any contamination and breakage even after 800K bonds
  In this respect, we are able to supply every customer with any type of Capillary with best delivery and price that no one can beat

## Slide 3
  Raw-material
  Woncosa Capillaries are formed out of an ultra pure 99.99% Alumina
  powder and Zirconia composite(AZ) material with special additives to
  make its density, hardness and fracture toughness more strong than any
  other products in the world
  Excellence of Woncosa Capillary
  Woncosa Capillary are capable of being used up to 1,200K bond at
  maximum in the production line without any yield loss and is also
  resistant to wear-out together with strong metalization
  As a result of this, Woncosa Capillary is best quality of the model being
  introduced in the market as of the moment
Woncosa Capillary is...

## Slide 4
Improve the material property
Improve the process and raise the density and hardness by ZrO2
* Comparative analysis the case of Al2O3+ZrO2 with and without ZrO2

## Slide 5
Comparing with others on material property
Hardness
(Gpa)

## Slide 6
Small Grain Growth
Average Size of Grain
Function of Zirconia(ZrO2) :
Restrain Al2O3 from strange growth
Zirconia provide protection the grain from the external stress for
the higher toughness property by Micro Crack
[ under 1㎛ ]

## Slide 7
Remove the pore of the FA by precise Grain Growth
Before improve
After improve

## Slide 8
FINE PITCH (bottleneck)
STANDARD
Capillary SEM Photos

## Slide 9
Capillary Manufacturing Process
FLOW - CHART 1
Powder
Mixing Powder
Dryness
Molding
Sintering
Al2O3 (99.99%), ZrO2
Ball Mill Process, Binder annexing
Spray Dryer Process
Oil Compression Molding
1500℃ ∼ 1650℃

## Slide 10
FLOW CHART 2
Blank
Outside Grinding
Length Cutting & Grinding
Classify by Hole Size
Outside Grinding
Center Grinding
STEP Grinding
Hole Grinding & Polishing

## Slide 11
Cone Grinding
FA Grinding
OR Grinding
Tip Polishing
IC Grinding
Final Inspection
Packing
Outside Grinding
FLOW-CHART 3

## Slide 12
Capillary Production Facilities
Capillary Automatic Grinding machine

## Slide 13
3D Non -Touchable Automatic inspection machine
Capillary Production Facilities

## Slide 14
Automatic Visual inspection machine
Capillary Production Facilities

## Slide 15
Process Test
Outside
Grinding
Length Cutting & Grinding
Classify by Hole Size
Cone
Grinding
FA
Grinding
OR
Grinding
IC
Grinding
Final
Inspection
Quality Control System
Outside diameter
(Φ 1.583)
Tip diameter
Cone angle
Cp, Cpk
Length
(11.1mm)
Face angle
OR
Cp,Cpk
CD, ICA
Cp, Cpk
Progress of work
Measured
QC Patrol Inspection
Inspection Cycle : 4th/Day
Progress of work
Measured
Depending on conditions

## Slide 16
Outgoing inspection
Cone Aangle,
TD
FA
OR
ICA, CD
Quality Control System
Inspection Item
Spec
Sampling
Application Of
Sampling Inspection by
Attributes
→ AQL
Spec of model

## Slide 17
Capillary Lifetime Evaluation
S.E.M Photos of Bond shape (Model : SZA18P-2000CF-74)
＜400k bonds＞
＜600k bonds＞
＜800k bonds＞

## Slide 18
Capillary Lifetime Evaluation
S.E.M Photos of capillary tip surface (Model : SZA18P-2000CF-74)
＜800k bonds＞
＜1,200k bonds＞

## Slide 19
1) Ball bonding problems
Hole size is too small.
Hole size is too large

## Slide 20
▶ Inner Chamfer angle is too large (120。 Over)
▶ CD dimension is too large
▶ This ball bond was made by a worn capillary
2) Ball bonding problems
▶ Chamfer diameter is too large

## Slide 21
Capacity Delivery
        Capacity
2003
2002
2001
2000
1999
10,000pcs
30,000pcs
60,000pcs
150,000pcs
250,000pcs
Capacity
        Delivery Plan
6 Working days
12 Working days
10 Working days
Delivery date
Rush Order
General Order
Sample
Item

## Slide 22
PLCC
SOJ
DIP
SOP
SSOP
MQFP
TSOP
TQFP
PGA
PBGA
SBGA
μBGA
Flex BGA
CSP
MLP
Wire:1.3mil
BPP:150㎛
Package Trend
Wire:1.2mil
BPP:100㎛
Wire:1.2-1.0mil
BPP:80㎛
Wire:1.0mil
BPP:60㎛
Wire:0.8mil
BPP:40㎛

## Slide 23
Bond Pad Pitch vs. Wire Diameter
PAD PITCH(um)
YEAR

## Slide 24
R & D Plan
      Bottleneck capillary for ultra fine BPP
30
40 ~ 35
50 ~ 40
2002
2001
2000
1999
Bigger than 50
BPP(㎛)
      Material development
2002
Ultra Extreme
Ceramic
Extreme Ceramic
2003
2001
2000
1999
Zirconia
&Alumina
Material

## Slide 25
Woncosa Capillary Life Time Evaluation

## Slide 31
Information for Woncosa Capillary Part No.

## Slide 32
Capillary Design Technology